Product Name:  ZT3632

Appearance:  A bronze satin gold color, free flowing powder with a bland luster.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                     33-41             12001-26-2             77019

Titanium Oxide(TiO2)            44-48             13463-67-7             77891

Iron(III) Oxide(Fe2O3)           15-29            1309-37-1             77891

Tin Oxide (SnO2)               <1              18282-10-5             77861

Pigment Green 7                <1               1328-53-6             74260

D50

Particle Size Distribution: 80% within the range5-25µm.        (By Malvern Mastersizer2000)

14.0±1.5

Visual and Colorimetric evaluation:    conforms                     KCPP

pH (10% Aqueous Suspension):	           4.0-9.0                     ISO787-9

Loss on Drying(105℃):	0.5% max.                  GB 5211.3-85

Oil Absorption:                     60-80 g oil/100g powder         GB 5211.15-88

Bulk Density:                       25-45 g/100cm3               GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)