Product Name:  Colour Series ZT3482

Appearance:   A shimmer peachblow color, free flowing powder with a bright pearl luster

Ingredients and Composition

Chemical Name               %                CAS No.              CI No.

Mica                    77-82               12001-26-2              77019

Titanium Oxide(TiO2)            18-23               13463-67-7              77891

Direct Red 80                 <1                  2610-10-8              35780

Pigment Red 112                <1                  6535-46-2              12370

D50

Particle Size Distribution: 80% within the range 10-100 µm.       (By Malvern Mastersizer2000)

41.0±3.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       15-40 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)