Product Name:  ZT3430

Appearance:   A glitter cupreous-Brown color, free flowing powder with a bright pearl luster.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                     74-80             12001-26-2             77019

Iron(III) Oxide(Fe2O3)             20-26             1309-37-1             77491

Pigment Black 7                 <1              1333-86-4             77266

D50

Particle Size Distribution: 80% within the range20-100µm.        (By Malvern Mastersizer2000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                     KCPP

pH (10% Aqueous Suspension):	           4.0-9.0                     ISO787-9

Loss on Drying(105℃):	0.5% max.                  GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder         GB 5211.15-88

Bulk Density:                       15-40 g/100cm3               GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)