Product Name:  ZT3426

Appearance:   A violaceous color, free flowing powder with a bright pearl luster.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                     39-48             12001-26-2             77019

Titanium Oxide(TiO2)            48-56             13463-67-7             77891

C.I.P.B15:3                   4-5               147-14-8               74160

D50

Particle Size Distribution: 80% within the range10-60µm.        (By Malvern Mastersizer3000E)

22±2

Visual and Colorimetric evaluation:    conforms                     KCPP

pH (10% Aqueous Suspension):	            5.0-9.0                     ISO787-9

Loss on Drying(105℃):	0.5% max.                  GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder         GB 5211.15-88

Bulk Density:                       15-40 g/100cm3               GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)