Product Name: Three Dimensional Super Interference Series SyaKarp 5G60A

Appearance: A free flowing off white powder with a bland pine green reflection color.

Ingredients and Composition

Chemical Name              %               CAS No.          CI No.

Mica                    35-45             12001-26-2          77019

Titanium Oxide(TiO2)             55-65             13463-67-7          77891

Tin Oxide (SnO2)                  <1               18282-10-5          77861

D50

Particle Size Distribution: 80% within the range 8-35 µm.       (By Malvern Mastersizer2000)

18.0±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           7.0 -10.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     70-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       20-40 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)