Product Name:  Exterior Brown-Green 9507WR

Appearance:  A brown-greencolor, free flowing powder with a bright metal luster

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                   56-60             12001-26-2             77019

Iron(III) Oxide(Fe2O3)             36-40             1309-37-1              77491

Cerium Oxide (Ce2O3)                <1               1345-13-7              77280

Polymer                   1-5

D50

Particle Size Distribution: 90% within the range 8-45µm.         (By Malvern Mastersizer2000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       15-35 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)