Product Name:  Exterior Brown Satin  9522WR

Appearance:  A brown satin color, free flowing powder with a bland metal luster.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                   42-48             12001-26-2             77019

Iron(III) Oxide(Fe2O3)             47-53             1309-37-1              77491

Cerium Oxide (Ce2O3)                <1               1345-13-7              77280

Polymer                   1-5

D50

Particle Size Distribution: 90% within the range 5-30µm.         (By Malvern Mastersizer2000)

14.0±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    GB 1717

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15

Bulk Density:                       15-35 g/100cm3              GB/T 23771

Density                            2.8-3.4 g / cm3 (water=1)