Product Name:  Exterior Sterling Silver  9103WR

Appearance:   An off-white color, free flowing powder with a pearl luster

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                    66-71             12001-26-2             77019

Titanium Oxide (TiO2)             23-28             13463-67-7             77891

Tin Oxide (SnO2)                   <1              18282-10-5             77861

Cerium Oxide (Ce2O3)                  <1              1345-13-7              77280

Polymer                    1-5

D50

Particle Size Distribution: 90% within the range (10-45) µm.       (By Malvern Mastersizer3000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    GB 1717

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15

Bulk Density:                       20-40 g/100cm3              GB/T 23771

Density                            2.8-3.4 g / cm3 (water=1)