Technical Data Sheet

| Product Name:1661 INCI Name: Synthetic Fluorphlogopite, Titanium Dioxide ，Silicon Dioxide and Tin Dioxide |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Composition |  | Specifications |  |  |  | Test Method |  |
| Synthetic Fluorphlogopite |  | 55-64% |  |  |  | ZTTM0307 |  |
| Titanium Dioxide |  | 10-14% |  |  |  | ZTTM0307 |  |
| Silicon Dioxide |  | 26-30% |  |  |  | ZTTM0307 |  |
| Tin Dioxide |  | 0-1% |  |  |  | ZTTM0307 |  |
| Appearance |  | Free flowing white powder |  |  |  | Visual |  |
| Particle Size |  | 20-200μm |  |  |  | ZTTM0301 |  |
| PH Value |  | 4-10 |  |  |  | ZTTM0304 |  |
| Odor |  | None |  |  |  | Organoleptic |  |
| Moisture |  | <1.0% |  |  |  | ZTTM0303 |  |
| Density |  | 2.8-3.4g/cm3 |  |  |  | ZTTM0306 |  |
| Oil Absorption |  | 50-85g/100g |  |  |  | ZTTM0305 |  |
| Heavy Metal |  |  |  |  |  |  |  |
| Composition | Specifications |  | Test Method | Composition | Specifications |  | Test Method |
| Pb | ＜10 |  | ZTTM0308 | Cd | ＜5 |  | ZTTM0308 |
| Hg | ＜1 |  | ZTTM0308 | Ni | ＜10 |  | ZTTM0308 |
| Sb | ＜10 |  | ZTTM0308 | Cr | ＜100 |  | ZTTM0308 |
| As | ＜2 |  | ZTTM0308 | Cu | ＜50 |  | ZTTM0308 |
| Zn | ＜50 |  | ZTTM0308 | Ba | ＜50 |  | ZTTM0308 |