Product Name:  CN862

Appearance:  A solar orange color, free flowing powder with a dazzling metal luster.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Synthetic Mica                 42-46             12003-38-2

Iron(III) Oxide(Fe2O3)             54-58             1309-37-1              77491

D50

Particle Size Distribution: 90% within the range10-45µm.        (By Malvern Mastersizer2000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                     KCPP

pH (10% Aqueous Suspension):	           4.0-7.0                    ISO787-9

Loss on Drying(105℃):	0.5% max.                  GB 5211.3-85

Oil Absorption:                     45-75 g oil/100g powder         GB 5211.15-88

Bulk Density:                       30-50 g/100cm3               GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)