Rayshine Super Silver

(Code: RH813)

INCI Name:                                    Calcium Aluminum Borosilicate, Silver

Chemical Composition:                                                                                                Test method

Calcium Aluminum Borosilicate                    67.0-70.0%                                              CLRTM-51

Ag                                                                     30.0-33.0%                                             CLRTM -48

Appearance                                                        silver                                                     CLRTM 52

Odor:                                                                 Odorless                                               CLRTM -52

Particle Size                                                      10-60μm                                               CLRTM -42

pH-Value (10% Aqueous Suspension):                      4.0-11.0                                               CLRTM -45

Oil Absorption                                            50.0-80.0 g/100g                                       CLRTM -46

Density                                                             2.8-3.4g/cm3                                                 CLRTM -47

Microbiology                                                   <100 cfu/g                                             CLRTM -54