SPECIFICATION

Cosray Rayspark Sparkle Gold

(Code: SP8721)

| INCI Name: | Calcium Aluminum Borosilicate, Titanium Dioxide, Tin Oxide |  |  |
| --- | --- | --- | --- |
| Chemical Composition: |  |  | Test method |
| Calcium Aluminum Borosilicate |  | 84.0-91.0% | CLRTM-51 |
| TiO2 |  | 9.0-15.0% | CLRTM-48 |
| SnO2 |  | ≤1.0% | CLRTM-48 |
| Appearance: |  | Sparkle Gold | CLRTM-52 |
| Odor: |  | Odorless | CLRTM-52 |
| Particle Size: |  | 100-700μm | CLRTM-42 |
| pH-Value(10% Aqueous Suspension): |  | 4.0-11.0 | CLRTM-45 |
| Oil Absorption: |  | 40.0-75.0g/100g | CLRTM-46 |
| Density |  | 2.4-2.9g/cm3 | CLRTM-47 |
| Microbiology: |  | <100 cfu/g | CLRTM-54 |
|  |  | No gram negative |  |
| Heavy Metals: |  |  | CLRTM -55 |
| As |  | <3ppm |  |
| Pb |  | <10ppm |  |
| Hg |  | <1ppm |  |
| Sb |  | <2ppm |  |
| Cd |  | <1ppm |  |

Zhongshan Zhongtai Pigment Co.,Ltd

Website: http://www.zsztyl.com	E-mail: zhongtaiyanliao@163.com