SPECIFICATION

Cosray Ray3D

MG5502-SF

| INCI Name: | Mica, Titanium Dioxide,Iron Oxide, Black Iron Oxide |  |  |
| --- | --- | --- | --- |
| Chemical Composition: |  |  | Test method |
| Mica |  | 41.0-51.0% | CLRTM -51 |
| Fe2O3 |  | 29.0-39.0% | CLRTM -48 |
| Fe3O4 |  | 15.0-25.0% | CLRTM -48 |
| Odor: |  | Odorless | CLRTM -53 |
| Particle Size: |  | 10-60μm | CLRTM -42 |
| pH-Value(10% Aqueous Suspension): |  | 4.0-11.0 | CLRTM-45 |
| Oil Absorption: |  | 40.0-95.0g/100g | CLRTM -46 |
| Density |  | 2.7-3.5g/cm3 | CLRTM -47 |
| Microbiology: |  | <100 cfu/g | CLRTM -54 |
|  |  | No gram negative |  |
| Heavy Metals: |  |  | CLRTM -55 |
| As |  | <3ppm |  |
| Pb |  | <10ppm |  |
| Hg |  | <1ppm |  |
| Sb |  | <2ppm |  |
| Cd |  | <5ppm |  |
| Zn |  | <100ppm |  |
| Ba |  | <50ppm |  |
| Cr |  | <100ppm |  |
| Cu |  | <50ppm |  |
| Ni |  | <200ppm |  |

Zhongshan Zhongtai Pigment Co.,Ltd

Website: http://www.zsztyl.com	E-mail: zhongtaiyanliao@163.com