Cosray Silk Black

(Code: 64126SF)

INCI Name:    Synthetic fluorphlogopite, Black Iron Oxide

Chemical Composition:                                                                                                Test method

Synthetic Mica                                                  28.0-38.0%                                           CLRTM-51

Black Iron Oxide                                              62.0-72.0%                                           CLRTM -48

Appearance:                                                        Black                                                 CLRTM -52

Odor:                                                                   Odorless                                             CLRTM -53

Particle Size:                                                       10-60µm                                            CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                  CLRTM-45

Oil Absorption:                                             50.0-90.0g/100g                                       CLRTM -46

Density                                                               2.5-3.5g/cm3                                               CLRTM -47

Microbiology:                                                 <100 cfu/g                                              CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                            <3ppm

Pb                                                                           <10ppm

Hg                                                                           <1ppm

Ba                                                                           <50ppm

Cd                                                                           <5ppm

Cr                                                                           <100ppm

Cu                                                                          <50ppm

Ni                                                                           <200ppm

Zn                                                                          <100ppm