Cosray Carbon Green

(Code: 4506F)

INCI Name:                                         Mica, Titanium Dioxide, Tin Oxide, Black Iron Oxide

Chemical Composition:                                                                                                Test method

Mica                                                                   37.0-55.0%                                           CLRTM-51

TiO2 (Rutile)                                                      42.0-48.0%                                           CLRTM -48

Black Iron Oxide                                              5.0-15.0%                                             CLRTM -48

SnO2                                                                 ≤ 1.0%                                                CLRTM -48     Appearance:                                             Blackish Green Powder                              CLRTM -52

Odor:                                                                   Odorless                                            CLRTM -53

Particle Size:                                                     10-60μm                                              CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM-45

Oil Absorption:                                             65.0-100.0g/100g                                    CLRTM -46

Density                                                               2.6-3.5g/cm3                                               CLRTM -47

Microbiology:                                                 <100 cfu/g                                              CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                      <1ppm

Sb                                                                       <2ppm

Cd                                                                      <5ppm

Zn                                                                      <100ppm

Ba                                                                      <50ppm

Cr                                                                       <100ppm

Cu                                                                      <50ppm

Ni                                                                       <200ppm