Cosray Carbon Gold

(Code: 4206F)

INCI Name:                                   Mica, Titanium Dioxide, Black Iron Oxide，Tin Oxide

Chemical Composition:                                                                                               Test method

Mica                                                                           37.0-56.0%                                CLRTM-51

TiO2                                                                           39.0-47.0%                                  CLRTM -48

Black Iron Oxide                                                      5.0-15.0%                                   CLRTM -48

SnO2                                                                                ≤1%                                    CLRTM -48

Appearance:                              Carbon Powder with Interference God                    CLRTM -52

Odor:                                                                   Odorless                                           CLRTM -53

Particle Size:                                                     10-60μm                                             CLRTM -42

pH-Value(10% Aqueous Suspension):             4.0-11.0                                              CLRTM-45

Oil Absorption:                                             50.0-90.0g/100g                                     CLRTM -46

Density                                                               2.9-3.6g/cm3                                             CLRTM -47

Microbiology:                                                 <100 cfu/g                                             CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                      <1ppm

Sb                                                                       <2ppm

Cd                                                                      <5ppm

Zn                                                                      <100ppm

Ba                                                                      <50ppm

Cr                                                                       <100ppm

Cu                                                                      <50ppm

Ni                                                                       <200ppm