Cosray Dark Black

(Code: 4601SF)

INCI Name:                                                        Mica, Black Iron Oxide,Titanium Dioxide

Chemical Composition:                                                                                                  Test method

Mica                                                                  30.0-44.0%                                           CLRTM-51

Black Iron Oxide                                              55.0-65.0%                                           CLRTM -48

TiO2                                                                  1.0-5.0%                                               CLRTM -48

Appearance:                                                     Black                                                     CLRTM -52

Odor:                                                                Odorless                                                CLRTM -53

Particle Size:                                                    10-60µm                                                CLRTM -42

pH-Value(10% Aqueous Suspension):          4.0-11.0                                                  CLRTM-45

Oil Absorption:                                               70.0-11.0g/100g                                     CLRTM -46

Density                                                            2.9-3.6g/cm3                                          CLRTM -47

Microbiology:                                                 <100 cfu/g                                              CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                     <1ppm

Sb                                                                     <2ppm

Cd                                                                     <5ppm

Zn                                                                     <100ppm

Ba                                                                      <50ppm

Cr                                                                     <100ppm

Cu                                                                     <50ppm

Ni                                                                      <200ppm