Cosray Blue Red

(Code: 4243RB)

INCI Name:  Mica, Titanium Dioxide,   FD&C Red 40 Al Lake

Chemical Composition:                                                                                               Test method

Mica                                                                   33.0-51.0%                                         CLRTM-51

TiO2 (Rutile)                                                      44.0-52.0%                                         CLRTM -48

FD&C Red 40 Al Lake                                     5.0-15.0%                                            CLRTM -48

Appearance:                                      Red Powder with Interference Blue                CLRTM -52

Odor:                                                                   Odorless                                           CLRTM -53

Particle Size:                                                     10-60μm                                             CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                CLRTM-45

Oil Absorption:                                             45.0-95.0g/100g                                     CLRTM -46

Density                                                               2.9-3.7g/cm3                                             CLRTM -47

Microbiology:                                                 <100 cfu/g                                             CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                         <3ppm

Pb                                                                        <20ppm

Hg                                                                       <1ppm

Sb                                                                       <2ppm

Cd                                                                      <1ppm

Zn                                                                      <50ppm