Cosray Orange Red

(Code: 4203R)

INCI Name:                                                  Mica, Titanium Dioxide, Tin Oxide, Red 40 Lake

Chemical Composition:                                                                                              Test method

Mica                                                                     37.0-56.0%                                        CLRTM-51

TiO2 (Rutile)                                                         39.0-47.0%                                      CLRTM -48

FD&C Red 40 Al Lake 2                                                5.0-15.0%                                         CLRTM -48

SnO2                                                                       ≤1%                                             CLRTM -48

Appearance:                                                 Orange Powder                                       CLRTM -52

Odor:                                                                   Odorless                                            CLRTM -53

Particle Size:                                                     10-60μm                                              CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM-45

Oil Absorption:                                             50.0-100.0g/100g                                     CLRTM -46

Density                                                               2.9-3.6g/cm3                                               CLRTM -47

Microbiology:                                                 <100 cfu/g                                              CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                         <3ppm

Pb                                                                        <20ppm

Hg                                                                       <1ppm

Sb                                                                       <2ppm

Cd                                                                      <1ppm

Zn                                                                      <50ppm