Cosray Rose Red

(Code: 4202R)

INCI Name:                                                  Mica, Titanium Dioxide, Tin Oxide, Red 27 Lake

Chemical Composition                                                                                             Test method

Mica                                                                      37.0-56.0%                                     CLRTM-51

TiO2 (Rutile)                                                          39.0-47.0%                                    CLRTM -48

FD&C Red 27 Al Lake                                           5.0-15.0%                                     CLRTM -48

SnO2                                                                            ≤1%                                        CLRTM -48

Appearance:                                                     Rosy Powder                                      CLRTM -52

Odor:                                                                   Odorless                                          CLRTM -53

Particle Size:                                                     10-60μm                                           CLRTM -42

pH-Value(10% Aqueous Suspension):             4.0-11.0                                            CLRTM-45

Oil Absorption:                                             70.0-110.0g/100g                                 CLRTM -46

Density                                                               2.7-3.2g/cm3                                          CLRTM -47

Microbiology:                                                 <100 cfu/g                                          CLRTM -54

No gram negative

Heavy Metals:                                                                                                            CLRTM -55

Arsenic(As)                                                      <3ppm

Lead(Pb)                                                          <20ppm

Mercury(Hg)                                                   <1ppm

Antimony(Sb)                                                 <2ppm

Cadmium(Cd)                                                 <1ppm

Zinc(Zn)                                                          <50ppm