Cosray Crystal Wine Red

(Code: 6573C)

INCI Name:                                            Synthetic fluorphlogopite, Iron Oxide

Chemical Composition:                                                                                                Test method

Synthetic Mica                                                71.0-82.0%                                              CLRTM-51

Fe2O3                                                               18.0-29.0%                                               CLRTM -48

Appearance:                                               Glitter Wine Red                                        CLRTM 52

Odor:                                                                Odorless                                                CLRTM -52

Particle Size:                                                   40-200μm                                               CLRTM -42

PH-Value (10% Aqueous Suspension):           4.0-11.0                                                CLRTM -45

Oil Absorption:                                          2.6-3.3g/100g                                              CLRTM -46

Density                                                             45-90g/cm3                                                  CLRTM -47

Microbiology:                                                <100 cfu/g                                               CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                               <3ppm

Pb                                                               <10ppm

Hg                                                              <1ppm

Sb                                                              <2ppm

Ba                                                             <50ppm

Cd                                                             <1ppm

Cr                                                              <100ppm

Cu                                                             <50ppm

Ni                                                              <200ppm

Zn                                                             <50ppm