Cosray Crystal Glitter Gold

(Code: 6335C)

INCI Name:   Synthetic fluorphlogopite, Titanium Dioxide, Iron Oxide,Tin Oxide

Chemical Composition:                                                                                               Test method

Synthetic fluorphlogopite                          40.0-59.0%                                                 CLRTM-51

TiO2                                                             35.0-55.0%                                                 CLRTM -48

Fe2O3                                                            5.0-15.0%                                                  CLRTM -48

SnO2                                                                  ≤1.0%                                                 CLRTM -48

Appearance:                                                 Golden                                                      CLRTM 52

Odor:                                                              Odorless                                                  CLRTM -52

Particle Size:                                                10-95μm                                                 CLRTM -42

pH-Value(10% Aqueous Suspension):        4.0-11.0                                                    CLRTM -45

Oil Absorption:                                          50.0-85.0g/100g                                          CLRTM -46

Density                                                             2.6-3.6g/cm3                                                CLRTM -47

Microbiology:                                                <100 cfu/g                                               CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                               <3ppm

Pb                                                               <10ppm

Hg                                                              <1ppm

Sb                                                              <2ppm

Ba                                                             <50ppm

Cd                                                             <1ppm

Cr                                                              <100ppm

Cu                                                             <50ppm

Ni                                                              <200ppm

Zn                                                             <50ppm