| COSRAY Pearsl: Royal Gold (Code:6305C ) |  |  |
| --- | --- | --- |
| ## Assay | ## Spec. Values | ## Test Method |
| ## Synthetic Mica | ## 24.0-55.0% | ## CLRTM-51 |
| ## TiO2 | ## 40.0-60.0% | ## CLRTM-48 |
| ## Fe2O3 | ## 5.0-15.0% | ## CLRTM-48 |
| ## SnO2 | ## ≤1.0% | ## CLRTM-48 |
| ## Particle Size | ## 10-60 µm | ## CLRTM-42 |
| ## PH Value | ## 4.0-11.0 | ## CLRTM-45 |
| ##### Density: | ## 2.7-3.7g/cm3 | ## CLRTM-47 |
| ## Oil absorption | 40.0-80.0g/100g | ## CLRTM-46 |
| Heavy Metals: |  | ## CLRTM -55 |
| As <3ppm Pb <10ppm Hg <1ppm Sb <2ppm Cd <1ppm Zn <50ppm Cr <100ppm Ni <200ppm |  |  |