Cosray Crystal Sparkle Violet

(Code: 6253C)

INCI Name:                                  Synthetic fluorphlogopite, Titanium Dioxide, Tin Oxide

Chemical Composition:                                                                                                Test method

Synthetic Mica                                         74.0-80.0 %                                                   CLRTM-51

TiO2                                                         19.0-25.0 %                                                   CLRTM -48

SnO2                                                            ≤1.0%                                                       CLRTM -48

Appearance:                                            Sparkle Violet                                               CLRTM 52

Odor:                                                            Odorless                                                    CLRTM -52

Particle Size:                                                 10-125μm                                                 CLRTM -42

pH-Value(10% Aqueous Suspension):        4.0-11.0                                                    CLRTM -45

Oil Absorption:                                          50-90g/100g                                               CLRTM -46

Density                                                            2.5-3.5 g/cm3                                                CLRTM -47

Microbiology:                                                <100 cfu/g                                               CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                     <1ppm

Sb                                                                      <2ppm

Cd                                                                     <1ppm

Zn                                                                     <50ppm