Cosray Sparkle Red Brown

(Code: 5052C)

INCI Name:                                                Mica, Iron Oxide

Chemical Composition:                                                                                                Test method

Mica                                                                  64.0-76.0%                                             CLRTM-51

Fe2O3                                                               24.0-36.0%                                            CLRTM -48

Appearance:                                              Sparkle Red Brown                                    CLRTM -52

Odor:                                                                  Odorless                                              CLRTM -53

Particle Size:                                                   10-125μm                                               CLRTM -42

Median size(D50):                                        40.0-80.0μm

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM -45

Oil Absorption:                                         50.0-110.0g/100g                                         CLRTM -46

Density                                                                2.7-3.6g/cm3                                              CLRTM -47

Microbiology:                                               <100 cfu/g

No gram negative                                         CLRTM -54

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                     <1ppm

Ba                                                                     <50ppm

Cd                                                                     <5ppm

Cr                                                                     <100ppm

Cu                                                                    <50ppm

Ni                                                                    <200ppm

Zn                                                                   <100ppm