Cosray Red Brown

(Code: 5002C)

INCI Name:                                                    Mica, Iron Oxide

Chemical Composition:                                                                                                Test method

Mica                                                                      48.0-61.0%                                        CLRTM-51

Fe2O3                                                                    39.0-52.0%                                        CLRTM -48

Appearance:                                                          Red Brown                                      CLRTM -52

Odor:                                                                     Odorless                                           CLRTM -53

Particle Size:                                                         10-60μm                                           CLRTM -42

Median size(D50):                                              16.0-28.0μm

pH-Value(10% Aqueous Suspension):               4.0-10.0                                             CLRTM -45

Oil Absorption:                                              40.0-85.0g/100g                                      CLRTM -46

Density                                                                2.8-3.7g/cm3                                              CLRTM -47

Microbiology:                                                    <100 cfu/g                                           CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                            <3ppm

Pb                                                                           <10ppm

Hg                                                                           <1ppm

Ba                                                                           <50ppm

Cd                                                                           <5ppm

Cr                                                                           <100ppm

Cu                                                                          <50ppm

Ni                                                                           <200ppm

Zn                                                                          <100ppm