| Technical Data Sheet Product Name:1645 INCI Name: Synthetic Fluorphlogopite, Titanium Dioxide ，Silicon Dioxide and Tin Dioxide |  |  |
| --- | --- | --- |
| Composition | Specifications | Test Method |
| Synthetic Fluorphlogopite | 31.2-52% | ZTTM0307 |
| Titanium Dioxide | 15-25% | ZTTM0307 |
| Silicon Dioxide | 33-43% | ZTTM0307 |
| Tin Dioxide | ≤0.8% | ZTTM0307 |
| Appearance | white powder | Visual |
| Particle Size | 15-75μm | ZTTM0301 |
| PH Value | 6-10 | ZTTM0304 |
| Odor | None | Organoleptic |
| Moisture | <1.0% | ZTTM0303 |
| Density | 2.2-3.2g/cm3 | ZTTM0306 |
| Oil Absorption | 60-120g/100g | ZTTM0305 |
| Heavy Metal |  |  |

| Composition | Specifications | Test Method | Composition | Specifications | Test Method |
| --- | --- | --- | --- | --- | --- |
| Pb | ＜10 | ZTTM0308 | Cd | ＜5 | ZTTM0308 |
| Hg | ＜1 | ZTTM0308 | Ni | ＜10 | ZTTM0308 |
| Sb | ＜10 | ZTTM0308 | Cr | ＜100 | ZTTM0308 |
| As | ＜2 | ZTTM0308 | Cu | ＜50 | ZTTM0308 |
| Zn | ＜50 | ZTTM0308 | Ba | ＜50 | ZTTM0308 |